Gambar 1. Hasil XRD (a=kaolin),(b=metakaolin),(c= AX2 zeolite),(d=modified AX2 zeolite),(e=  AX4 zeolite),(f= modified AX4 zeolite),(g= AZ zeolite), (h= modified AZ3 zeolite).

f

e

d

c

b

a

Gambar 2. Hasil SEM (a= AX2 zeolite), (b = modified AX2 zeolite ), (c= AX4 zeolite), (d= modified AX4 zeolite), (e= AZ3zeolite), (f= modified AZ3 zeolite )

Tabel 1 perbandingan volume dalam sintesis zeolit

| Sampel | Volume (ml) |  |
| --- | --- | --- |
|  | Kaolin | Na2SiO3 (Merck) |
| Sampel AX1 | 40 | 60 |
| Sampel AX2 | 50 | 50 |
| Sampel AX3 | 60 | 40 |
| Sampel AX4 | 90 | 10 |

Tabel 2 Perbandingan volume sintesis zeolit AZ

| Sampel | Volume (ml) |  |
| --- | --- | --- |
|  | Kaolin | Na-Aluminat |
| Sampel AZ1 | 40 | 60 |
| Sampel AZ2 | 50 | 50 |
| Sampel AZ3 | 60 | 40 |

Tabel 3. Kapasitas adsorpsi  Cu(II) and Biru Metilena

| Sample | Adsorption capacity for methylene blue (mg/g) | Adsorption capacity for Cu (II) (mg/g) | Adsorption Isotherm type |
| --- | --- | --- | --- |
| Zeolit Y | 18,44 | 1,53 | Langmuir (R2=0,9755) |
| Zeolite Y modified by MPTS | 17,31 | 1,40 | Langmuir (R2=0,9929) |
| Mixture Zeolit A and sodalite | 27,68 | 1,59 | Langmuir (R2=0,9872) |
| sodalite modified by MPTS | 28,82 | 1,62 | Langmuir (R2=0,9596) |
| Zeolit A | 17,81 | 1,44 | Langmuir (R2=0,9530) |
| Zeolite A by MPTS | 30,114 | 1,63 | Langmuir (R2=0,9969) |